Client: EMLab P&K (QA)
C/O: Mr. Quality Control
Re: Sample Report	Date of Sampling: 01-10-2013
Date of Receipt: 01-10-2013
Date of Report: 01-10-2013	

ASBESTOS PLM REPORT

Location:	7	
Comments (see below)	A	
Lab ID-Version‡:	4534286-1	
Sample Layers	Asbestos Content	
White Drywall	ND	
White Joint Compound	2% Chrysotile	
Tape	ND	
White Compound with Paint	ND	
Composite Asbestos Fibrous Content: 	< 1% Asbestos	
Composite Non-Asbestos Content: 	20% Cellulose	
Sample Composite Homogeneity: 	Good	

Comments: A) Composite asbestos content provided is only for Drywall/Joint compound. Composite content provided does not follow the guidelines set forth by NVLAP.  This analysis was performed by following the NESHAP guidelines.

Location:	8	
Comments (see below)	None	
Lab ID-Version‡:	4534287-1	
Sample Layers	Asbestos Content	
Black Mastic	2% Chrysotile	
Gray Floor Tile	4% Chrysotile	
Sample Composite Homogeneity: 	Good	

Comments: 

Location:	9	
Comments (see below)	None	
Lab ID-Version‡:	4534288-1	
Sample Layers	Asbestos Content	
Brown Ceiling Tile	< 1% Chrysotile	
Sample Composite Homogeneity: 	Good	

Comments: 

The test report shall not be reproduced except in full, without written approval of the laboratory. The report must not be used by the client to claim product certification, approval, or endorsement by NVLAP, NIST, or any agency of the federal government. The Company reserves the right to dispose of all samples after a period of thirty (30) days, according to all state and federal guidelines, unless otherwise specified.

 Inhomogeneous samples are separated into homogeneous subsamples and analyzed individually. ND means no fibers were detected. When detected, the minimum detection and reporting limit is less than 1% unless point counting is performed. 
‡ A "Version" indicated by -"x" after the Lab ID# with a value greater than 1 indicates a sample with amended data.  The revision number is reflected by the value of "x".